**US ORIGIN**

Terms and Conditions
Commodity: Green Delayed Petroleum Coke
Grade: 4.5% sulfur
Origin: USGC
Laycan: TBA
Quantity: 30,000 MT (+/- 10%) Can increase per mutual agreement
Loading: Galveston, Texas
Price: TBA FOB
Contract Term: 12 months with extensions up to three (3) years
Specs:
As Received Dry Basis Moisture 7.74 -- Ash % 0.38 0.41 VM % 10.01 10.85 Fixed Carbon % 81.81 88.74 Sulfur 4.40 4.77 Nitrogen 1.49 1.62 Net BTU/lb 13,818 15,064 Net CV Kcal/lb 7,676 8,369 HGI 67
Bulk Density lb/ cu ft 52.7

**SAUDI ORIGIN**

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **PARAMETER** |  | **UNIT** |  | **ARB** |  | **DB** |  | **ADB** |
|  |  |  |  |  |  |  |  |  |
| Gross Calorific Value |   | Kcal/Kg |   | 7700 |   | 8400 |   | 8300 |
| Net Calorific Value |   | Kcal/Kg |   | 7461 |   | 8202 |   | 8142 |
| Total Moisture |   | PCT |   | 8.44 |   |   |   |   |
| Moisture in analysis sample |   | PCT |   |   |   |   |   | 0.68 |
| Ash |   | PCT |   | 0.27 |   | 0.29 |   | 0.29 |
| Volatile Matter |   | PCT |   | 9.14 |   | 9.98 |   | 9.91 |
| Fixed Carbon |   | PCT |   | 82.16 |   | 89.73 |   | 89.12 |
| Sulphur |   | PCT |   | 7.45 |   | 8.14 |   | 8.08 |
| HGI |   | POINT |   |   |   |   |   | 56 |
|   |   |   |   |   |   |   |   |   |
| **SIZE FRACTIONS** |  | **RESULTS** |
| Above 50 mm |   | 5.43 |
| 0 - 50 mm |   | 94.57 |