**US ORIGIN**

Terms and Conditions  
Commodity: Green Delayed Petroleum Coke  
Grade: 4.5% sulfur  
Origin: USGC  
Laycan: TBA  
Quantity: 30,000 MT (+/- 10%) Can increase per mutual agreement  
Loading: Galveston, Texas  
Price: TBA FOB  
Contract Term: 12 months with extensions up to three (3) years  
Specs:  
As Received Dry Basis Moisture 7.74 -- Ash % 0.38 0.41 VM % 10.01 10.85 Fixed Carbon % 81.81 88.74 Sulfur 4.40 4.77 Nitrogen 1.49 1.62 Net BTU/lb 13,818 15,064 Net CV Kcal/lb 7,676 8,369 HGI 67  
Bulk Density lb/ cu ft 52.7

**SAUDI ORIGIN**

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **PARAMETER** |  | **UNIT** |  | **ARB** |  | **DB** |  | **ADB** |
|  |  |  |  |  |  |  |  |  |
| Gross Calorific Value |  | Kcal/Kg |  | 7700 |  | 8400 |  | 8300 |
| Net Calorific Value |  | Kcal/Kg |  | 7461 |  | 8202 |  | 8142 |
| Total Moisture |  | PCT |  | 8.44 |  |  |  |  |
| Moisture in analysis sample |  | PCT |  |  |  |  |  | 0.68 |
| Ash |  | PCT |  | 0.27 |  | 0.29 |  | 0.29 |
| Volatile Matter |  | PCT |  | 9.14 |  | 9.98 |  | 9.91 |
| Fixed Carbon |  | PCT |  | 82.16 |  | 89.73 |  | 89.12 |
| Sulphur |  | PCT |  | 7.45 |  | 8.14 |  | 8.08 |
| HGI |  | POINT |  |  |  |  |  | 56 |
|  |  |  |  |  |  |  |  |  |
| **SIZE FRACTIONS** |  | **RESULTS** | | | | | | |
| Above 50 mm |  | 5.43 | | | | | | |
| 0 - 50 mm |  | 94.57 | | | | | | |